G.N.-403A

BITUMINOUS SURFACE TREATMENTS: The resulting target application rates are as follows:

SHOULDER SEAL:

| TYPE OF CONSTRUCTION | BITUMINOUS MATERIAL | APPLICATION RATE | AGGREGATE | APPLICATION RATE |
| --- | --- | --- | --- | --- |
| A-1 | HFE-CRSP | 0.25 gal/yd2 | FM-01 (SPECIAL) | 15 lb/yd2 |
| A-1 | HFE-CRSP | 0.25 gal/yd2 | FM-20 (SPECIAL) | 15 lb/yd2 |

AGGREGATE GRADATION:

TOTAL PERCENT PASSING

| SIEVE NUMBER | FM-01 (SPECIAL) | FM-20 (SPECIAL) |
| --- | --- | --- |
| 3/8” | 100 | 100 |
| No.4 | 97+/-3 | 97+/-3 |
| No.8 | 85+/-15 | 70+/-20 |
| No.16 | 40+/-15 | 40+/-15 |
| No.50 | 12+/-12 | 12+/-12 |
| No.100 | 8+/-8 | 8+/-8 |
| No.200 | 1.5+/-1 | 1.5+/-1 |
| DESCRIPITON | WET BOTTOM BOILER SLAG | CRUSHED GRAVEL |

NOTE:  THE ENGINEER RESERVES THE RIGHT TO ADJUST THE TARGET APPLICATION RATES AND THE QUANTITIES.

DESIGN NOTES:  (Design notes shall not appear in the contract.)

- The Bituminous Materials and Application Rates shall be verified with Materials Section in Project Implementation during plan preparation.

- The applicable information on this sheet should be included in the General Notes for the contract.