# LONGITUDINAL JOINT DENSITY (D5-FG)

Eff.:  January 1, 2010

Rev.:    July 15, 2013

Description.  This work shall consist of testing the density of longitudinal joints as part of the quality control/quality assurance (QC/QA) of hot-mix asphalt (HMA).  Work shall be according to Section 1030 of the Standard Specifications except as follows.

Quality Control/Quality Assurance (QC/QA).  Delete the second and third sentence of the third paragraph of Article 1030.05(d)(3) of the Standard Specifications.

Add the following paragraphs to the end of Article 1030.05(d)(3) of the Standard Specifications:

“	Longitudinal joint density testing shall be performed at each random density test location.  Longitudinal joint testing shall be located at a distance equal to the lift thickness or a minimum of  4 in. ( 100 mm), from each pavement edge.  (i.e. for a 4 in. (100 mm) lift the near edge of the density gauge or core barrel shall be within 4 in. (100 mm) from the edge of pavement.)  Longitudinal joint density testing shall be performed using either a correlated nuclear gauge or cores.

a.	Confined Edge.  Each confined edge density shall be represented by a one-minute nuclear density reading or a core density and shall be included in the average of density readings or core densities taken across the mat which represents the Individual Test.

b.	Unconfined Edge.  Each unconfined edge joint density shall be represented by an average of three one-minute density readings or a single core density at the given density test location and shall meet the density requirements specified herein.  The three one-minute readings shall be spaced ten feet apart longitudinally along the unconfined pavement edge and centered at the random density test location.”

Revise the Density Control Limits table in Article 1030.05(d)(4) of the Standard Specifications to read:

| “Mixture Composition | Parameter | Individual Test (includes confined edges) | Unconfined Edge Joint Density Minimum |
| --- | --- | --- | --- |
| IL-4.75 | Ndesign=50 | 93.0 – 97.4% 1/ | 90.0% |
| IL-9.5, IL-12.5 | Ndesign ≥ 90 | 92.0 – 96.0% | 90.0% |
| IL-9.5,IL-9.5L,IL-12.5 | Ndesign < 90 | 92.5 – 97.4% | 90.0% |
| IL-19.0,IL-19.0FG, IL-25.0 | Ndesign ≥ 90 | 93.0 – 96.0% | 90.0% |
| IL-19.0, IL-19.0FG,IL-19.0L,IL-25.0 | Ndesign < 90 | 93.0 – 97.4% | 90.0% |
| IL-9.5FG < 1 ¼ in (32 mm) | Ndesign = 50 - 105 | 90.0 – 95.0% | 90.0% |
| IL-9.5FG > 1 ¼ in (32 mm) | Ndesign = 50 - 105 | 92.0 – 96.0% | 90.0% |
| SMA | Ndesign = 50 & 80 | 93.5 – 97.4% | 91.0% |
| All Other | Ndesign = 30 | 93.02 - 97.4% | 90.0% |

1/  	Density shall be determined by cores or by correlated, approved thin lift gauge.

2/	92.0% when placed as first lift on an unimproved subgrade.

103005(d)(3)-2