# IL 19.0 BINDER DENSITY REQUIREMENT WHEN PLACING < 2.25”

Eff. 05-15-2006

Rev. 09-01-2006

For all IL 19.0 Binder mix placed the required density control limits will be 92.0 – 96.0%.

40616.doc