All Regional Engineers

Eric E. Harm

Special Provision for Reflective Sheeting on Channelizing Devices

July 25, 2008

This special provision was developed by the Bureau of Operations and the Bureau of Materials and Physical Research to update the channelizing device sheeting specifications to current standards.  It has been revised to tie the color of the reflective sheeting to standard color tolerance charts.

This special provision should be inserted in all construction contracts.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the November 7, 2008, and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory July 25, 2008.

80183m

# reflective sheeting ON CHANNELIZING DEVICES (BDE)

Effective:  April 1, 2007

Revised:  November 1, 2008

Revise the seventh paragraph of Article 1106.02 of the Standard Specifications to read:

“	At the time of manufacturing, the retroreflective prismatic sheeting used on channelizing devices shall meet or exceed the initial minimum coefficient of retroreflection as specified in the following table.  Measurements shall be conducted according to ASTM E 810, without averaging.  Sheeting used on cones, drums and flexible delineators shall be reboundable as tested according to ASTM D 4956.  Prestriped sheeting for rigid substrates on barricades shall be white and orange.  The sheeting shall be uniform in color and devoid of streaks throughout the length of each roll.  The color shall conform to the latest appropriate standard color tolerance chart issued by the U.S. Department of Transportation, Federal Highway Administration, and to the daytime and nighttime color requirements of ASTM D 4956.

| Initial Minimum Coefficient of Retroreflection candelas/foot candle/sq ft (candelas/lux/sq m) of material |  |  |  |  |
| --- | --- | --- | --- | --- |
| Observation Angle (deg.) | Entrance Angle (deg.) | White | Orange | Fluorescent Orange |
| 0.2 | -4 | 365 | 160 | 150 |
| 0.2 | +30 | 175 | 80 | 70 |
| 0.5 | -4 | 245 | 100 | 95 |
| 0.5 | +30 | 100 | 50 | 40” |

Revise the first sentence of the first paragraph of Article 1106.02(c) of the Standard Specifications to read:

“	Barricades and vertical panels shall have alternating white and orange stripes sloping downward at 45 degrees toward the side on which traffic will pass.”

Revise the third sentence of the first paragraph of Article 1106.02(d) of the Standard Specifications to read:

“	The bottom panels shall be 8 x 24 in. (200 x 600 mm) with alternating white and orange stripes sloping downward at 45 degrees toward the side on which traffic will pass.”

80183