All Regional Engineers

Charles J. Ingersoll

Special Provision for Hot-Mix Asphalt – Plant Test Frequency

September 25, 2009

This special provision was developed by the Bureau of Materials and Physical Research to bring the Quality Control testing frequency more in line with nationwide standards.

It should be inserted in HMA contracts.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the January 15, 2010 letting and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory September 25, 2009.

80201m

# hot-mix asphalt – plant test frequency (BDE)

Effective:  April 1, 2008

Revised:  January 1, 2010

Revise the table in Article 1030.05(d)(2)a. of the Standard Specifications to read:

| “Parameter | Frequency of Tests High ESAL Mixture Low ESAL Mixture | Frequency of Tests All Other Mixtures | Test Method See Manual of Test Procedures for Materials |
| --- | --- | --- | --- |
| Aggregate Gradation % passing sieves: 1/2 in. (12.5 mm), No. 4 (4.75 mm), No. 8 (2.36 mm), No. 30 (600 m) No. 200 (75 m) Note 1. | 1 washed ignition oven test on the mix per half day of production Note 4. | 1 washed ignition oven test on the mix per day of production Note 4. | Illinois Procedure |
| Asphalt Binder Content by Ignition Oven Note 2. | 1 per half day of production | 1 per day | Illinois-Modified AASHTO T 308 |
| VMA Note 3. | Day’s production ≥ 1200 tons: 1 per half day of production | N/A | Illinois Modified AASHTO R 35 |
|  | Day’s production < 1200 tons: 1 per half day of production for first 2 days and 1 per day thereafter (first sample of the day) |  |  |
| Air Voids Bulk Specific Gravity of Gyratory Sample | Day’s production ≥ 1200 tons: 1 per half day of production | 1 per day | Illinois-Modified AASHTO T 312 |
|  | Day’s production < 1200 tons: 1 per half day of production for first 2 days and 1 per day thereafter (first sample of the day) |  |  |
| Maximum Specific Gravity of Mixture | Day’s production ≥ 1200 tons: 1 per half day of production | 1 per day | Illinois-Modified AASHTO T 209 |
|  | Day’s production < 1200 tons: 1 per half day of production for first 2 days and 1 per day thereafter (first sample of the day) |  |  |

Note 1.  The No. 8 (2.36 mm) and No. 30 (600 m) sieves are not required for All Other Mixtures.

Note 2.  The Engineer may waive the ignition oven requirement for asphalt binder content if the aggregates to be used are known to have ignition asphalt binder content calibration factors which exceed 1.5 percent.  If the ignition oven requirement is waived, other Department approved methods shall be used to determine the asphalt binder content.

Note 3.  The Gsb used in the voids in the mineral aggregate (VMA) calculation shall be the same average Gsb value listed in the mix design.

Note 4.  The Engineer reserves the right to require additional hot bin gradations for batch plants if control problems are evident.”

80201