All Regional Engineers

Eric E. Harm

Special Provision for Hot-Mix Asphalt – Transportation

January 11, 2008

This special provision was developed by the Bureau of Materials and Physical Research to provide an alternative to truck bed release agents when transporting HMA.  It should be inserted in all HMA contracts.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the April 25, 2008, and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory 
January 11, 2008.

80202m

# hot-mix asphalt – transportation (BDE)

Effective:  April 1, 2008

Revise Article 1030.08 of the Standard Specifications to read:

“	1030.08	Transportation.  Vehicles used in transporting HMA shall have clean and tight beds.  The beds shall be sprayed with asphalt release agents from the Department’s approved list.  In lieu of a release agent, the Contractor may use a light spray of water with a light scatter of manufactured sand (FA 20 or FA 21) evenly distributed over the bed of the vehicle.  After spraying, the bed of the vehicle shall be in a completely raised position and it shall remain in this position until all excess asphalt release agent or water has been drained.

When the air temperature is below 60 ºF (15 ºC), the bed, including the end, endgate, sides and bottom shall be insulated with fiberboard, plywood or other approved insulating material and shall have a thickness of not less than 3/4 in (20 mm).  When the insulation is placed inside the bed, the insulation shall be covered with sheet steel approved by the Engineer.  Each vehicle shall be equipped with a cover of canvas or other suitable material meeting the approval of the Engineer which shall be used if any one of the following conditions is present.

(a)	Ambient air temperature is below 60 ºF (15 ºC).

(b)	The weather is inclement.

(c)	The temperature of the HMA immediately behind the paver screed is below 250 ºF (120 ºC).

The cover shall extend down over the sides and ends of the bed for a distance of approximately 12 in. (300 mm) and shall be fastened securely.  The covering shall be rolled back before the load is dumped into the finishing machine.”

80202