All Regional Engineers

Scott E. Stitt

Special Provision for Above Grade Inlet Protection

September 30, 2011

This special provision was developed by the Illinois Development Council and Bureau of Design and Environment to provide designers with another means of protecting inlet structures from sediment.  It has been revised to fit with the 2012 Standard Specifications.

It should be inserted in contracts at the district’s discretion.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the January 20, 2012 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory September 30, 2011.

80240m

# above grade inlet protection (BDE)

Effective:  July 1, 2009

Revised:  January 1, 2012

Add the following to Article 280.02 of the Standard Specifications:

“(m)	Above Grade Inlet Filter 	1081.15(j)”

Add the following paragraph after the second paragraph of Article 280.04(c) of the Standard Specifications:

“When above grade inlet filters are specified, they shall be of sufficient size to completely span and enclose the inlet structure.  Prior to ordering materials, the Contractor shall determine the size of the various drainage structures being protected.”

Add the following paragraph after the second paragraph of Article 280.08(d) of the Standard Specifications:

“Protection of drainage structures with rigid inlet protection assemblies will be paid for at the contract unit price per each for ABOVE GRADE INLET FILTERS.”

Add the following to Article 1081.15 of the Standard Specifications:

“(j)	Above Grade Inlet Filters.  Above grade inlet filters shall consist of a rigid polyethylene frame covered with a fitted geotextile filter.  A clean, used fitted filter and a used rigid polyethylene frame in good condition meeting the approval of the Engineer may be substituted for new materials.  Materials for the above grade inlet filter assembly shall be according to the following.

(1)	Frame Construction.  Frame shall be constructed of a high density polyethylene copolymer.  The design of the frame shall allow the structure to fit completely over the sewer inlet.  The frame shall be a minimum of 26 in. (650 mm) tall and the top of the frame shall be designed with an opening to allow large volumes of water to pass through under high flow events.  The frame shall conform to the following requirements:

| Frame |  |  |
| --- | --- | --- |
| Material Property | Test Method | Value |
| Tensile Yield Strength | ASTM D 638 | 3600 psi (24.82 MPa) |
| Elongation at Break | ASTM D 638 | >600% |
| Tensile-Impact Strength | ASTM D 1822 | 170 ft lb/sq in (230 J) |
| Brittleness Temperature | ASTM D 746 | <-105°F (-76.11°C) |
| Environmental Stress Cracking | ASTM D 1693 | >800 hours |
| Durometer Hardness, Shore A | ASTM D 2240 | 68 |

| Vicat Softening Temperature | ASTM D 1525 | 254°F (123.33°C) |
| --- | --- | --- |
| Deflection Temperature | ASTM D 648 | 157°F (69.44°C) |
| Coefficient of Linear Thermal Expansion | ASTM D 696 | 7x10-5 in/in/°F (12.6x10-5 m/m/°C) |
| Bulk Density | ASTM D 1895 | 37 lbs/cu ft (592.7 kg/cu m) |

(2)	Fitted Geotextile Filter.  The sides of the fitted geotextile filter shall be constructed of 100 percent continuous polyester needle-punched fabric.  The filter shall be fabricated to provide a direct fit to the frame.  The top of the filter shall integrate a coarse screening to allow large volumes of water to pass through in the event of heavy flows.  This screening shall have a minimum apparent opening of 1/2 in. (13 mm).  The filter shall have integrated anti-buoyancy pockets capable of holding no less than 3.0 cu ft (0.08 cu m) of stabilization material.  Each filter shall have a label with the following information sewn to or otherwise permanently adhered to the outside: manufacturer’s name, product name, and lot, model or serial number.  The fitted geotextile filter shall conform to the following requirements:

| Fitted Geotextile Filter |  |  |
| --- | --- | --- |
| Material Property | Test Method | Minimum Avg. Roll Value |
| Weight | ASTM D 3776 | 3.0 oz/sq yd +/- 10% (71.1 grams/sq m) |
| Grab Tensile Strength | ASTM D 4632 | 80 lb min. (36.29 kg) |
| Grab Tensile Elongation | ASTM D 4632 | 50% |
| Bursting Strength | ASTM D 3786 | 150 psi min. (1.03 MPa) |
| Puncture Resistance | ASTM D 4833 | 50 lb min. (22.68 kg) |
| Trapezoid Tearing Strength | ASTM D 4533 | 30 lb min. (13.61 kg) |
| Apparent Opening Size | ASTM D 4751 | Sieve No. 70 (0.212 mm) |
| Permittivity | ASTM D 4491 | 2.0/sec |
| Water Permeability | ASTM D 4491 | 102 gal/min/sq ft (4150 liter/min/sq m) |
| UV Resistance | ASTM D 4355 | 70% at 500 hours |

(3)	Certification.  The manufacturer shall furnish a certificate with each shipment of above grade inlet filter assemblies, stating the amount of product furnished and that the material complies with these requirements.”

80240