All Regional Engineers

John D. Baranzelli

Special Provision for Coarse Aggregate in Bridge Approach Slabs/Footings

January 11, 2013

This special provision was developed by the Bureau of Materials and Physical Research to clarify the aggregate materials used in precast bridge approach slabs and precast pavement.  It has been revised to further clarify the requirements.

This special provision should be inserted into contracts with bridge approach slabs and bridge approach footings.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the April 26, 2013 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory 
January 11, 2013.

80292m

# coarse aggregate in bridge approach slabs/footings (bde)

Effective:  April 1, 2012

Revised:  April 1, 2013

Revise the third paragraph of Article 1004.01(b) of the Standard Specifications to read:

“	Aggregates used in Class BS concrete (except when poured on subgrade), Class PS concrete, and Class PC concrete (bridge superstructure products only, excluding the approach slab) shall contain no more than two percent by weight (mass) of deleterious materials.  Deleterious materials shall include substances whose disintegration is accompanied by an increase in volume which may cause spalling of the concrete.”

Revise the first sentence of the first paragraph of Article 1004.02(f) of the Standard Specifications to read:

“	(f)	Freeze-Thaw Rating.  When coarse aggregate is used to produce portland cement concrete for base course, base course widening, pavement (including precast), driveway pavement, sidewalk, shoulders, curb, gutter, combination curb and gutter, median, paved ditch, concrete superstructures on subgrade such as bridge approach slabs (excluding precast), concrete structures on subgrade such as bridge approach footings, or their repair using concrete, the gradation permitted will be determined from the results of the Department’s Freeze-Thaw Test (Illinois Modified AASHTO T 161).”

80292