All Regional Engineers

Omer M. Osman, P.E.

Special Provision for Hot-Mix Asphalt – Mixture Design Composition and Volumetric Requirements

July 25, 2014

This special provision was developed by the Bureau of Materials and Physical Research to 1) define an acceptable range of air voids for determining acceptability of a test strip, 2) revise the minimum percent passing the #8 sieve requirements for IL-9.5 surface mixtures, 3) increase the VMA requirement to 15.0 percent for IL-9.5 surface mixtures, and 4) add in the missing field VMA control limits for IL-4.75 mixtures.

It has been revised to eliminate IL-25.0, IL-12.5 surface mixture, N105 mixtures and “All Other” (i.e. BAM) mixtures and to make IL-19.0 a finer gradation mixture.  It has also been revised to delete the Constructing Test Strip pay item.

This special provision should be inserted into all HMA contracts.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the November 7, 2014 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory July 25, 2014.

80322m

# hot-mix asphalt – mixture design composition and volumetric requirements (bde)

Effective:  November 1, 2013

Revised:  November 1, 2014

Revise the last sentence of the first paragraph of Article 312.05 of the Standard Specifications to read:

“	The minimum compacted thickness of each lift shall be according to Article 406.06(d).”

Delete the minimum compacted lift thickness table in Article 312.05 of the Standard Specifications.

Revise the second paragraph of Article 355.02 of the Standard Specifications to read:

“	The mixture composition used shall be IL-19.0.”

Revise Article 355.05(a) of the Standard Specifications to read:

“	(a)	The top lift thickness shall be 2 1/4 in. (60 mm) for mixture composition IL-19.0.”

Revise the Leveling Binder table and second paragraph of Article 406.05(c) of the Standard Specifications to read:

| “Leveling Binder |  |
| --- | --- |
| Nominal, Compacted, Leveling Binder Thickness, in. (mm) | Mixture Composition |
| ≤ 1 1/4 (32) | IL-4.75, IL-9.5, or IL-9.5L |
| > 1 1/4 to 2 (32 to 50) | IL-9.5 or IL-9.5L |

The density requirements of Article 406.07(c) shall apply for leveling binder, machine method, when the nominal compacted thickness is:  3/4 in. (19 mm) or greater for 
IL-4.75 mixtures; and 1 1/4 in. (32 mm) or greater for IL-9.5 and IL-9.5L mixtures.”

Revise the table in Article 406.06(d) of the Standard Specifications to read:

| “MINIMUM COMPACTED LIFT THICKNESS |  |
| --- | --- |
| Mixture Composition | Thickness, in. (mm) |
| IL-4.75 | 3/4 (19) |
| IL-9.5, IL-9.5L | 1 1/4 (32) |
| SMA-12.5 | 1 1/2 (38) |
| IL-19.0, IL-19.0L | 2 1/4 (57)” |

Revise the ninth paragraph of Article 406.14 of the Standard Specifications to read:

“Test strip mixture will be evaluated at the contract unit price according to the following.”

Revise Article 406.14(a) of the Standard Specifications to read:

“	(a)	If the HMA placed during the initial test strip is determined to be acceptable the mixture will be paid for at the contract unit price.”

Revise Article 406.14(b) of the Standard Specifications to read:

“	(b)	If the HMA placed during the initial test strip (1) is determined to be unacceptable to remain in place by the Engineer, and (2) was not produced within 2.0 to 6.0 percent air voids or within the individual control limits of the JMF according to the Department’s test results, the mixture will not be paid for and shall be removed at the Contractor’s expense.  An additional test strip shall be constructed and the mixture will be paid for in full, if produced within 2.0 to 6.0 percent air voids and within the individual control limits of the JMF.”

Revise Article 406.14(c) of the Standard Specifications to read:

“	(c)	If the HMA placed during the initial test strip (1) is determined to be unacceptable to remain in place by the Engineer, and (2) was produced within 2.0 to 6.0 percent air voids and within the individual control limits of the JMF according to the Department’s test results, the mixture shall be removed.  Removal will be paid according to Article 109.04.  This initial mixture will be paid for at the contract unit price.  An additional test strip shall be constructed and the mixture will be paid for in full, if produced within 2.0 to 6.0 percent air voids and within the individual control limits of the JMF.”

Delete Article 406.14(d) of the Standard Specifications.

Delete Article 406.14(e) of the Standard Specifications.

Delete the last sentence of Article 407.06(c) of the Standard Specifications.

Revise Note 2. of Article 442.02 of the Standard Specifications to read:

“	Note 2.  The mixture composition of the HMA used shall be IL-19.0 binder, designed with the same Ndesign as that specified for the mainline pavement.”

Delete the second paragraph of Article 482.02 of the Standard Specifications.

Revise the first sentence of the sixth paragraph of Article 482.05 of the Standard Specifications to read:

“	When the mainline HMA binder and surface course mixture option is used on resurfacing projects, shoulder resurfacing widths of 6 ft (1.8 m) or less may be placed simultaneously with the adjacent traffic lane for both the binder and surface courses.”

Revise the second sentence of the fourth paragraph of Article 601.04 of the Standard Specifications to read:

“	The top 5 in. (125 mm) of the trench shall be backfilled with an IL-19.0L Low ESAL mixture meeting the requirements of Section 1030 and compacted to a density of not less than 90 percent of the theoretical density.”

Revise the second sentence of the fifth paragraph of Article 601.04 of the Standard Specifications to read:

“	The top 8 in. (200 mm) of the trench shall be backfilled with an IL-19.0L Low ESAL mixture meeting the requirements of Section 1030 and compacted to a density of not less than 90 percent of the theoretical density.”

Revise Article 1003.03(c) of the Standard Specifications to read:

“	(c)	Gradation.  The fine aggregate gradation for all HMA shall be FA 1, FA 2, FA 20, FA 21, or FA 22.  The fine aggregate gradation for SMA shall be FA/FM 20.

For mixture IL-4.75 and surface mixtures with an Ndesign = 90, at least 50 percent of the required fine aggregate fraction shall consist of either stone sand, slag sand, or steel slag meeting the FA 20 gradation.

For mixture IL-19.0, Ndesign = 90 the fine aggregate fraction shall consist of at least 67 percent manufactured sand meeting FA 20 or FA 22 gradation.  For mixture IL-19.0, Ndesign = 50 or 70 the fine aggregate fraction shall consist of at least 50 percent manufactured sand meeting FA 20 or FA 22 gradation.  The manufactured sand shall be stone sand, slag sand, steel slag sand, or combinations thereof.

Gradation FA 1, FA 2, or FA 3 shall be used when required for prime coat aggregate application for HMA.”

Remove footnote 3/ from the tables and at the end of the tables in Article 1004.01(c) of the Standard Specifications.

Delete the last sentence of the first paragraph of Article 1004.03(b) of the Standard Specifications.

Revise the table in Article 1004.03(c) of the Standard Specifications to read:

| “Use | Size/Application | Gradation No. |
| --- | --- | --- |
| Class A-1, 2, & 3 | 3/8 in. (10 mm) Seal | CA 16 |
| Class A-1 | 1/2 in. (13 mm) Seal | CA 15 |
| Class A-2 & 3 | Cover | CA 14 |
| HMA High ESAL | IL-19.0 IL-9.5 | CA 11 1/ CA 16 and/or CA 13 CA 16 |
| HMA Low ESAL | IL-19.0L IL-9.5L Stabilized Subbase or Shoulders | CA 11 1/ CA 16 |

1/	CA 16 or CA 13 may be blended with the gradations listed.”

Revise the nomenclature table in Article 1030.01 of the Standard Specifications to read:

| “High ESAL | IL-19.0 binder; IL-9.5 surface |
| --- | --- |
| Low ESAL | IL-19.0L binder; IL-9.5L surface; Stabilized Subbase (HMA)1/; HMA Shoulders2/ |

1/	Uses 19.0L binder mix.

2/	Uses 19.0L for lower lifts and 9.5L for surface lift.”

Revise Article 1030.02 of the Standard Specifications and Supplemental Specifications to read:

“1030.02	Materials.  Materials shall be according to the following.

Item	Article/Section

(a)	Coarse Aggregate 	1004.03

(b)	Fine Aggregate 	1003.03

(c)	RAP Material 	1031

(d)	Mineral Filler 	1011

(e)	Hydrated Lime 	1012.01

(f)	Slaked Quicklime (Note 1)

(g)	Performance Graded Asphalt Binder (Note 2) 	1032

(h)	Fibers (Note 3)

(i)	Warm Mix Asphalt (WMA) Technologies (Note 4)

Note 1.  Slaked quicklime shall be according to ASTM C 5.

Note 2.  The asphalt binder shall be an SBS PG 76-28 when the SMA is used on a full-depth asphalt pavement and SBS PG 76-22 when used as an overlay.

Note 3.  A stabilizing additive such as cellulose or mineral fiber shall be added to the SMA mixture according to Illinois Modified AASHTO M 325.  The stabilizing additive shall meet the Fiber Quality Requirements listed in Illinois Modified AASHTO M 325.  Prior to approval and use of fibers, the Contractor shall submit a notarized certification by the producer of these materials stating they meet these requirements.

Note 4.  Warm mix additives or foaming processes shall be selected from the current Bureau of Materials and Physical Research Approved List, “Warm Mix Asphalt Technologies”.”

Revise Article 1030.04(a)(1) of the Standard Specifications and the Supplemental Specifications to read:

“	(1)	High ESAL Mixtures.  The Job Mix Formula (JMF) shall fall within the following limits.

| High ESAL, MIXTURE COMPOSITION (% PASSING) 1/ |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sieve Size | IL-19.0 mm |  | SMA 12.5 4/ |  | IL-9.5 mm |  | IL-4.75 mm |  |
|  | min | max | min | max | min | max | min | max |
| 1 1/2 in (37.5 mm) |  |  |  |  |  |  |  |  |
| 1 in. (25 mm) |  | 100 |  |  |  |  |  |  |
| 3/4 in. (19 mm) | 90 | 100 |  | 100 |  |  |  |  |
| 1/2 in. (12.5 mm) | 75 | 89 | 90 | 99 |  | 100 |  | 100 |
| 3/8 in. (9.5 mm) |  |  | 50 | 85 | 90 | 100 |  | 100 |
| #4 (4.75 mm) | 40 | 60 | 20 | 40 | 32 | 69 | 90 | 100 |
| #8 (2.36 mm) | 26 | 42 | 16 | 24 5/ | 32 | 52 2/ | 70 | 90 |
| #16 (1.18 mm) | 15 | 30 |  |  | 10 | 32 | 50 | 65 |
| #50 (300 µm) | 6 | 15 |  |  | 4 | 15 | 15 | 30 |
| #100 (150 µm) | 4 | 9 |  |  | 3 | 10 | 10 | 18 |
| #200 (75 µm) | 3 | 6 | 8.0 | 11.0 3/ | 4 | 6 | 7 | 9 |
| Ratio Dust/Asphalt Binder |  | 1.0 |  |  |  | 1.0 |  | 1.0 3/ |

1/	Based on percent of total aggregate weight.

2/	The mixture composition shall not exceed 44 percent passing the #8 (2.36 mm) sieve for surface courses with Ndesign = 90.

3/	Additional minus No. 200 (0.075 mm) material required by the mix design shall be mineral filler, unless otherwise approved by the Engineer.

4/	The maximum percent passing the #635 (20 µm) sieve shall be ≤ 3 percent.

5/	When establishing the Adjusted Job Mix Formula (AJMF) the percent passing the #8 (2.36 mm) sieve shall not be adjusted above 24 percent.”

Delete Article 1030.04(a)(3) of the Standard Specifications.

Delete Article 1030.04(a)(4) of the Standard Specifications.

Revise the table in Article 1030.04(b)(1) of the Standard Specifications to read:

| “VOLUMETRIC REQUIREMENTS High ESAL |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Voids in the Mineral Aggregate (VMA), % minimum |  |  | Voids Filled with Asphalt Binder (VFA), % |
| Ndesign | IL-19.0 | IL-9.5 | IL-4.751/ |  |
| 50 | 13.5 | 15.0 | 18.5 | 65 – 78 2/ |
| 70 |  |  |  | 65 - 75 |
| 90 |  |  |  |  |

1/	Maximum Draindown for IL-4.75 shall be 0.3 percent

2/	VFA for IL-4.75 shall be 76-83 percent”

Revise the table in Article 1030.04(b)(2) of the Standard Specifications to read:

| “VOLUMETRIC REQUIREMENTS Low ESAL |  |  |  |  |
| --- | --- | --- | --- | --- |
| Mixture Composition | Design Compactive Effort | Design Air Voids Target % | VMA (Voids in the Mineral Aggregate), % min. | VFA (Voids Filled with Asphalt Binder), % |
| IL-9.5L | NDES =30 | 4.0 | 15.0 | 65-78 |
| IL-19.0L | NDES =30 | 4.0 | 13.5 | N/A” |

Replace Article 1030.04(b)(3) of the Standard Specifications with the following:

“(3)	SMA Mixtures.

| ESALs (million) | Ndesign | Design Air Voids Target % | Voids in the Mineral Aggregate (VMA), % min. | Voids Filled with Asphalt (VFA), % |
| --- | --- | --- | --- | --- |
| £ 10 | 50 | 4.0 | 16.0 | 75 – 80 |
| > 10 | 80 | 4.0 | 17.0 | 75 – 80” |

Delete Article 1030.04(b)(4) of the Standard Specifications.

Delete Article 1030.04(b)(5) from the Supplemental Specifications.

Revise the table in Article 1030.05(d)(2)a. of the Standard Specifications to read:

| “Parameter | Frequency of Tests High ESAL Mixture Low ESAL Mixture | Test Method See Manual of Test Procedures for Materials |
| --- | --- | --- |
| Aggregate Gradation % passing sieves: 1/2 in. (12.5 mm), No. 4 (4.75 mm), No. 8 (2.36 mm), No. 30 (600 µm) No. 200 (75 µm) | 1 washed ignition oven test on the mix per half day of production Note 3. | Illinois Procedure |
| Asphalt Binder Content by Ignition Oven Note 1. | 1 per half day of production | Illinois-Modified AASHTO T 308 |
| VMA Note 2. | Day’s production ≥ 1200 tons: 1 per half day of production | Illinois-Modified AASHTO R 35 |
|  | Day’s production < 1200 tons: 1 per half day of production for first 2 days and 1 per day thereafter (first sample of the day) |  |
| Air Voids Bulk Specific Gravity of Gyratory Sample Note 4. | Day’s production ≥ 1200 tons: 1 per half day of production | Illinois-Modified AASHTO T 312 |
|  | Day’s production < 1200 tons: 1 per half day of production for first 2 days and 1 per day thereafter (first sample of the day) |  |
| Maximum Specific Gravity of Mixture | Day’s production ≥ 1200 tons: 1 per half day of production | Illinois-Modified AASHTO T 209 |
|  | Day’s production < 1200 tons: 1 per half day of production for first 2 days and 1 per day thereafter (first sample of the day) |  |

Note 1.  The Engineer may waive the ignition oven requirement for asphalt binder content if the aggregates to be used are known to have ignition asphalt binder content calibration factors which exceed 1.5 percent.  If the ignition oven requirement is waived, other Department approved methods shall be used to determine the asphalt binder content.

Note 2.  The Gsb used in the voids in the mineral aggregate (VMA) calculation shall be the same average Gsb value listed in the mix design.

Note 3.  The Engineer reserves the right to require additional hot bin gradations for batch plants if control problems are evident.

Note 4.  The WMA compaction temperature for mixture volumetric testing shall be 270 ± 5 °F (132 ± 3 °C) for quality control testing.  The WMA compaction temperature for quality assurance testing will be 270 ± 5 °F (132 ± 3 °C) if the mixture is not allowed to cool to room temperature.  If the mixture is allowed to cool to room temperature, it shall be reheated to standard HMA compaction temperatures.”

Revise the table in Article 1030.05(d)(2)b. of the Standard Specifications to read:

| “Parameter | High ESAL Mixture Low ESAL Mixture |
| --- | --- |
| Ratio Dust/Asphalt Binder | 0.6 to 1.2 |
| Moisture | 0.3 %” |

Revise the Article 1030.05(d)(4) of the Supplemental Specifications to read:

“	(4)	Control Limits.  Target values shall be determined by applying adjustment factors to the AJMF where applicable.  The target values shall be plotted on the control charts within the following control limits.

| CONTROL LIMITS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Parameter | High ESAL Low ESAL |  | SMA |  | IL-4.75 |  |
|  | Individual Test | Moving Avg. of 4 | Individual Test | Moving Avg. of 4 | Individual Test | Moving Avg. of 4 |
| % Passing: 1/ |  |  |  |  |  |  |
| 1/2 in. (12.5 mm) | ± 6 % | ± 4 % | ± 6 % | ± 4 % |  |  |
| 3/8 in. (9.5mm) |  |  | ± 4 % | ± 3 % |  |  |
| No. 4 (4.75 mm) | ± 5 % | ± 4 % | ± 5 % | ± 4 % |  |  |
| No. 8 (2.36 mm) | ± 5 % | ± 3 % | ± 4 % | ± 2 % |  |  |
| No. 16 (1.18 mm) |  |  | ± 4 % | ± 2 % | ± 4 % | ± 3 % |
| No. 30 (600 µm) | ± 4 % | ± 2.5 % | ± 4 % | ± 2.5 % |  |  |
| Total Dust Content No. 200 (75 µm) | ± 1.5 % | ± 1.0 % |  |  | ± 1.5 % | ± 1.0 % |
| Asphalt Binder Content | ± 0.3 % | ± 0.2 % | ± 0.2 % | ± 0.1 % | ± 0.3 % | ± 0.2 % |
| Voids | ± 1.2 % | ± 1.0 % | ± 1.2 % | ± 1.0 % | ± 1.2 % | ± 1.0 % |
| VMA | -0.7 % 2/ | -0.5 % 2/ | -0.7 % 2/ | -0.5 % 2/ | -0.7 % 2/ | -0.5 % 2/ |

1/	Based on washed ignition oven

2/	Allowable limit below minimum design VMA requirement

| DENSITY CONTROL LIMITS |  |  |
| --- | --- | --- |
| Mixture Composition | Parameter | Individual Test |
| IL-4.75 | Ndesign = 50 | 93.0 - 97.4 % 1/ |
| IL-9.5 | Ndesign = 90 | 92.0 - 96.0 % |
| IL-9.5,IL-9.5L | Ndesign < 90 | 92.5 - 97.4 % |
| IL-19.0 | Ndesign = 90 | 93.0 - 96.0 % |
| IL-19.0, IL-19.0L | Ndesign < 90 | 93.0 2/- 97.4 % |
| SMA | Ndesign = 50 & 80 | 93.5 - 97.4 % |

1/	Density shall be determined by cores or by correlated, approved thin lift nuclear gauge.

2/	92.0 % when placed as first lift on an unimproved subgrade.”

Revise the table in Article 1030.05(d)(5) of the Supplemental Specifications to read:

| “CONTROL CHART REQUIREMENTS | High ESAL, Low ESAL, SMA & IL-4.75 |
| --- | --- |
| Gradation 1/ 3/ | % Passing Sieves: 1/2 in. (12.5 mm) 2/ No. 4 (4.75 mm) No. 8 (2.36 mm) No. 30 (600 µm) |
| Total Dust Content 1/ | No. 200 (75 µm) |
|  | Asphalt Binder Content |
|  | Bulk Specific Gravity |
|  | Maximum Specific Gravity of Mixture |
|  | Voids |
|  | Density |
|  | VMA |

1/	Based on washed ignition oven.

2/	Does not apply to IL-4.75.

3/	SMA also requires the 3/8 in. (9.5 mm) sieve.”

Delete Article 1030.05(d)(6)a.1.(b.) of the Standard Specifications.

Delete Article 1030.06(b) of the Standard Specifications.

Delete Article 1102.01(e) of the Standard Specifications.

80322