All Regional Engineers

Omer M. Osman, P.E.

Special Provision for Retroreflective Sheeting for Highway Signs

July 25, 2014

This special provision was developed by the Bureau of Materials and Physical Research and Bureau of Operations to update the requirements for the coefficient of retroreflection to allow averaging of the 0 degree and 90 degree rotational angles.  This follows the industry standard and the ASTM E 810 test method.  This allows multiple manufacturers to meet each of the sheeting specifications and makes Type ZZ sheeting eligible for Federal funding.

This special provision should be inserted into all contracts having retroreflective sheeting on highway signs.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the November 7, 2014 and subsequent lettings. The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory July 25, 2014.

80350m

# retroreflective sheeting for highway signs (BDE)

Effective:  November 1, 2014

Revise the first sentence of the first paragraph of Article 1091.03(a)(3) of the Standard Specifications to read:

“	When tested according to ASTM E 810, with averaging, the sheeting shall have a minimum coefficient of retroreflection as show in the following tables.”

Replace the Tables for Type AA sheeting, Type AP sheeting, Type AZ sheeting and Type ZZ sheeting in Article 1091.03(a)(3) with the following.

Type AA Sheeting

Minimum Coefficient of Retroreflection

Candelas/foot candle/sq ft (candelas/lux/sq m) of material

Type AA (Average of 0 and 90 degree rotation)

| Observation Angle (deg.) | Entrance Angle (deg.) | White | Yellow | Red | Green | Blue | FO |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.2 | -4 | 800 | 600 | 120 | 80 | 40 | 200 |
| 0.2 | +30 | 400 | 300 | 60 | 35 | 20 | 100 |
| 0.5 | -4 | 200 | 150 | 30 | 20 | 10 | 75 |
| 0.5 | +30 | 100 | 75 | 15 | 10 | 5 | 35 |

Type AA (45 degree rotation)

| Observation Angle (deg.) | Entrance Angle (deg.) | Yellow | FO |
| --- | --- | --- | --- |
| 0.2 | -4 | 500 | 165 |
| 0.2 | +30 | 115 | 40 |
| 0.5 | -4 | 140 | 65 |
| 0.5 | +30 | 60 | 30 |

Type AP Sheeting

Minimum Coefficient of Retroreflection

Candelas/foot candle/sq ft (candelas/lux/sq m) of material

Type AP (Average of 0 and 90 degree rotation)

| Observation Angle (deg.) | Entrance Angle (deg.) | White | Yellow | Red | Green | Blue | Brown | FO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.2 | -4 | 500 | 380 | 75 | 55 | 35 | 25 | 150 |
| 0.2 | +30 | 180 | 135 | 30 | 20 | 15 | 10 | 55 |
| 0.5 | -4 | 300 | 225 | 50 | 30 | 20 | 15 | 90 |
| 0.5 | +30 | 90 | 70 | 15 | 10 | 7.5 | 5 | 30 |

Type AZ Sheeting

Minimum Coefficient of Retroreflection

Candelas/foot candle/sq ft (candelas/lux/sq m) of material

Type AZ (Average of 0 and 90 degree rotation)

| Observation Angle (deg.) | Entrance Angle (deg.) | White | Yellow | Red | Green | Blue | FYG | FY |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.2 | -4 | 375 | 280 | 75 | 45 | 25 | 300 | 230 |
| 0.2 | +30 | 235 | 170 | 40 | 25 | 15 | 190 | 150 |
| 0.5 | -4 | 245 | 180 | 50 | 30 | 20 | 200 | 155 |
| 0.5 | +30 | 135 | 100 | 25 | 15 | 10 | 100 | 75 |
| 1.0 | -4 | 50 | 37.5 | 8.5 | 5 | 2 | 45 | 25 |
| 1.0 | +30 | 22.5 | 20 | 5 | 3 | 1 | 25 | 12.5 |

Type ZZ Sheeting

Minimum Coefficient of Retroreflection

Candelas/foot candle/sq ft (candelas/lux/sq m) of material

Type ZZ (Average of 0 and 90 degree rotation)

| Observation Angle (deg.) | Entrance Angle (deg.) | White | Yellow | Red | Green | Blue | FYG | FY | FO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.2 | -4 | 570 | 425 | 90 | 60 | 30 | 460 | 340 | 170 |
| 0.2 | +30 | 190 | 140 | 35 | 20 | 10 | 150 | 110 | 65 |
| 0.5 | -4 | 400 | 300 | 60 | 40 | 20 | 320 | 240 | 120 |
| 0.5 | +30 | 130 | 95 | 20 | 15 | 7 | 100 | 80 | 45 |
| 1.0 | -4 | 115 | 90 | 17 | 12 | 5 | 95 | 70 | 35 |
| 1.0 | +30 | 45 | 35 | 7 | 5 | 2 | 35 | 25 | 15 |

80350