# PFP QUALITY LEVEL ANALYSIS (HMAFG D5)

Eff. 06-29-11

Revise the table for Pay Attributes and Price Adjustment Factors in the PFP Quality Level Analysis included in Appendix E1 of the Manual of Test Procedures for Materials to read as follows:

| Table 1: Pay Attributes and Price Adjustment Factors |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Measured Attribute |  | Factor “f” | UL | LL |  |
| VMA |  | 0.3 | MDR1/ +3.0 | MDR1/ _ 0.7 |  |
| Plant Voids |  | 0.3 | Design Voids + 1.35 | Design Voids - 1.35 |  |
|  | In-Place Density IL 4.75 IL19.0,19.0FG & 25.0 SMA | 0.4 | 97.02/ | 91.52/ |  |
|  |  | 0.4 | 97.0 | 92.5 |  |
|  |  | 0.4 | 97.0 | 92.2 |  |
|  |  | 0.4 | 98.0 | 93.0 |  |

1.  MDR=Minimum Density Requirement

2.  Applies to all HMA mixes other than IL-4.75, IL-19.0, IL-19.0FG, IL-25.0, and SMA

HMA FG