# HOT-MIX ASPHALT MIXTURE IL-19.0FG

Effective:  December 1, 2009

Revised:    October 12, 2011

Description.  This work shall consist of constructing fine graded hot-mix asphalt (HMA) binder course with an IL-19.0FG mixture.  Work shall be according to Sections 406, 407 and 1030 of the Standard Specifications, except as modified herein.

Materials.  Revise Article 1003.03(c) of the Standard Specifications to read:

“(c)	Gradation.  The fine aggregate gradation for all HMA shall be FA 1, FA 2, FA 20, FA 21,or FA 22.  For mixture IL-19.0FG, the fine aggregate fraction shall consist of at least 67 percent manufactured sand meeting FA 20, FA 21 or FA 22 gradation.  The manufactured sand shall be stone sand, slag sand, steel slag sand, or combinations thereof.”

The coarse aggregate shall be the same as those specified on the table in Article 1004.03 for IL-19.0 mixtures.

Gradation FA 1, FA 2, or FA 3 shall be used when required for prime coat aggregate application for HMA.

Mixture Design.  Add the following to the table in Article 1030.04(a)(1):

| “High ESAL, MIXTURE COMPOSITION (% PASSING) 1/ |  |  |
| --- | --- | --- |
| Sieve Size | IL-19.0FG |  |
|  | min | max |
| 1 1/2 in (37.5 mm) |  |  |
| 1 in. (25 mm) |  | 100 |
| 3/4 in. (19 mm) | 90 | 100 |
| 1/2 in. (12.5 mm) | 69 | 89 |
| 3/8 in. (9.5 mm) |  |  |
| #4 (4.75 mm) | 45 | 60 |
| #8 (2.36 mm) | 30 | 45 |
| #16 (1.18 mm) | 20 | 35 |
| #30 (600 m) |  |  |
| #50 (300 m) | 8 | 15 |
| #100 (150 m) | 6 | 9 |
| #200 (75 m) | 3.5 | 5.5 |
| Ratio Dust/Asphalt Binder |  | 1.0 |

Revise the table in Article 1030.04(b)(1) of the Standard Specifications to read:

|  | “VOLUMETRIC REQUIREMENTS High ESAL |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Voids in the Mineral Aggregate (VMA), % minimum |  |  |  | Voids Filled with Asphalt Binder (VFA), % |
| Ndesign | IL-25.0 | IL-19.0 | IL-19.0FG | IL-12.5 | IL-9.5 |  |
| 50 | 12.0 | 13.0 | 13.5 | 14.0 | 15 | 65 - 78 |
| 70 |  |  |  |  |  | 65 - 75 |
| 90 |  |  |  |  |  |  |
| 105 |  |  |  |  |  |  |

Quality Control/Quality Assurance (QC/QA).  Revise the second table in Article       1030.05(d)(4) to read:

| DENSITY CONTROL LIMITS |  |  |
| --- | --- | --- |
| Mixture Composition | Parameter | Individual Test |
| IL-4.75 | Ndesign = 50 | 93.0 – 97.4% 1/ |
| IL-9.5, IL-12.5 | Ndesign ≥ 90 | 92.0 – 96.0 % |
| IL-9.5, IL-9.5L, IL-12.5 | Ndesign < 90 | 92.5 – 97.4 % |
| IL-19.0, IL-19.0FG, IL-25.0 | Ndesign ≥ 90 | 93.0 – 96.0 % |
| IL-19.0, IL-19.0FG, IL-19.0L, IL-25.0 | Ndesign < 90 | 93.0 – 97.4 % |
| All Other | Ndesign = 30 | 93.0 2 - 97.4 % |

1/	Density shall be determined by cores or by correlated, approved thin lift gauge.

2/   92.0 % when placed as first lift on an unimproved subgrade.

Basis of Payment.  Add the following two paragraphs after the third paragraph of Article 406.14 of the Standard Specifications:

Mixture IL-19.0FG will be paid for at the contract unit price per ton (metric ton) for HOT-MIX ASPHALT BINDER COURSE, IL-19.0FG, of the Ndesign specified.

Mixture IL-19.0FG in which polymer modified asphalt binders are required will be paid for at the contract unit price per ton (metric ton) for POLYMERIZED HOT-MIX ASPHALT BINDER COURSE, IL-19.0FG, of the Ndesign specified.”

HMA IL-19 0 FG