# WEATHERING STEEL PLATE BEAM GUARDRAIL AND POST

Effective:  Unknown						Revised:  November 1, 2006

This special provision sets forth revisions to Standard 630001 for STEEL PLATE BEAM GUARDRAIL AND POST.

All guardrail rail elements on this contract and post shall be of the weathering steel type and shall conform to the requirements of AASHTO M180, M222, and the Standard Specifications.  Steel posts shall be Grade A.  All mounting hardware, end shoes and accessories shall be of the standard type as shown on the Standards and as specified in the Standard Specifications.

All standard galvanized surfaces which are exposed to view by traffic shall be painted after erection in accordance with the Special Provision for WEATHERED BROWN GUARDRAIL PAINT.  Care shall be taken so that weathered steel surfaces are not covered by paint and any weathered surfaces so covered shall be cleaned in accordance with the manufacturer's recommendations.

At all metal to metal contact surfaces, including faying areas and bolting points, where other than galvanized to galvanized contact occurs, a 1" (25 mm) soft plastic or nylon washer shall be placed.  The washer shall be 1/16" (1.5mm) thick and shall be dark brown in color.

Only Weathering Steel Post shall be used on this project except Breakaway Post with driven Tubular Steel Foundations shall be used where required.

The Weathering Steel Post shall be painted from its bottom to a point which will be 6 in (150 mm) above the ground line.  This work will be done according to the appropriate portions of the Special Provisions for WEATHERED BROWN GUARDRAIL PAINT and Section 506 of the Standard Specifications.  Painting the posts and all the work and materials involved will not be paid for separately, but shall be considered included in WEATHERING STEEL PLATE BEAM GUARDRAIL.

The guardrail shall be reflectorized in accordance with the PRISMATIC GUARDRAIL REFLECTORS Special Provision.

This work shall be paid for at the contract unit price per foot (meter) for WEATHERING STEEL PLATE BEAM GUARDRAIL of the type specified measured according to Article 630.07 of the Standard Specifications.