# HOT-MIX ASPHALT SHOULDERS, SPECIAL

Eff. 03-09-2001 								Rev. 01-01-2014

In addition to the requirements of Articles 406 and 1030 of the Standard Specifications the following restrictions shall apply.

The coarse aggregate for the Hot-Mix Asphalt Shoulders, Special shall be crushed gravel meeting the gradation requirement for CA-16.  The crushed gravel must contain a minimum of 40% hard particles (siliceous and/or igneous) by weight.  The Department must approve the aggregate for this mixture.  The coarse aggregate shall be blended with natural sand, FA-01/02 and/or crushed gravel sand, FA-20 to meet the requirements for an IL9.5, N50 mixture per article 1030.04(a)(1).  A maximum of 10% Recycled Asphalt Pavement (RAP) will be allowed in the mixture.

This work will be paid for at the contract unit price per ton (metric ton) for HOT-MIX ASPHALT SHOULDERS, SPECIAL.

482C.doc