Regional Engineers

Omer M. Osman

Special Provision for Aggregate Subgrade Improvement

January 8, 2016

This special provision was developed by the Bureau of Materials and Physical Research to allow the use of gravel in fills over 24 inches in thickness.  This special provision has been revised to fit with the 2016 Standard Specifications.

The designer should check with the District Geotechnical Engineer to determine the appropriate thickness of the aggregate subgrade material.

When this special provision is used, BDE special provision, “Reclaimed Asphalt Pavement (RAP) and Reclaimed Asphalt Shingles (RAS)” should also be included in the contract.

It should be included in all contracts utilizing aggregate subgrade improvements.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the April 22, 2016 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory 
January 8, 2016.

80274m

# aggregate subgrade improvement (bde)

Effective:  April 1, 2012

Revised:  April 1, 2016

Add the following Section to the Standard Specifications:

“SECTION 303.  AGGREGATE SUBGRADE IMPROVEMENT

303.01	Description.  This work shall consist of constructing an aggregate subgrade improvement.

303.02	Materials.  Materials shall be according to the following.

Item	Article/Section

(a)	Coarse Aggregate 	1004.07

(b)	Reclaimed Asphalt Pavement (RAP) (Notes 1, 2, and 3) 	1031

Note 1.  Crushed RAP, from either full depth or single lift removal, may be mechanically blended with aggregate gradations CS 01, CS 02, and RR 01 but shall not exceed 40 percent of the total product.  The top size of the RAP shall be less than 4 in. (100 mm) and well graded.

Note 2.  RAP having 100 percent passing the 1 1/2 in. (37.5 mm) sieve and being well graded, may be used as capping aggregate in the top 3 in. (75 mm) when aggregate gradations CS 01, CS 02, or RR 01 are used in lower lifts.

Note 3. The RAP used for aggregate subgrade improvement shall be according to the current Bureau of Materials and Physical Research Policy Memorandum, “Reclaimed Asphalt Pavement (RAP) for Aggregate Applications”.

303.03	Equipment.  The vibratory machine shall be according to Article 1101.01, or as approved by the Engineer.

303.04	Soil Preparation.  The stability of the soil shall be according to the Department’s Subgrade Stability Manual for the aggregate thickness specified.

303.05	Placing Aggregate.  The maximum nominal lift thickness of aggregate gradations CA 02, CA 06, or CA 10 shall be 12 in. (300 mm).  The maximum nominal lift thickness of aggregate gradations CS 01, CS 02, and RR 01 shall be 24 in. (600 mm).

303.06	Capping Aggregate.  The top surface of the aggregate subgrade shall consist of a minimum 3 in. (75 mm) of aggregate gradations CA 06 or CA 10.  When the contract specifies that a granular subbase is to be placed on the aggregate subgrade improvement, the 3 in. (75 mm) of capping aggregate shall be the same gradation and may be placed with the underlying aggregate subgrade improvement material.

303.07	Compaction.  All aggregate lifts shall be compacted to the satisfaction of the Engineer.  If the moisture content of the material is such that compaction cannot be obtained, sufficient water shall be added so that satisfactory compaction can be obtained.

303.08	Finishing and Maintenance of Aggregate Subgrade Improvement.  The aggregate subgrade improvement shall be finished to the lines, grades, and cross sections shown on the plans, or as directed by the Engineer.  The aggregate subgrade improvement shall be maintained in a smooth and compacted condition.

303.09	Method of Measurement.  This work will be measured for payment according to Article 311.08.

303.10	Basis of Payment.  This work will be paid for at the contract unit price per cubic yard (cubic meter) or ton (metric ton) for AGGREGATE SUBGRADE IMPROVEMENT or at the contract unit price per square yard (square meter) for AGGREGATE SUBGRADE IMPROVEMENT, of the thickness specified.”

Add the following to Section 1004 of the Standard Specifications:

“	1004.07	Coarse Aggregate for Aggregate Subgrade Improvement.  The aggregate shall be according to Article 1004.01 and the following.

(a)	Description.  The coarse aggregate shall be crushed gravel, crushed stone, or crushed concrete.  In applications where greater than 24 in. (600 mm) of subgrade material is required, gravel may be used below the first 12 in (300 mm) of subgrade.

(b)	Quality.  The coarse aggregate shall consist of sound durable particles reasonably free of deleterious materials.

(c)	Gradation.

(1)	The coarse aggregate gradation for total subgrade thickness less than or equal to 12 in. (300 mm) shall be CA 2, CA 6, CA 10, or CS 01.

The coarse aggregate gradation for total subgrade thickness more than 12 in. (300 mm) shall be CS 01 or CS 02 as shown below or RR 01 according to Article 1005.01(c).

|  | COARSE AGGREGATE SUBGRADE GRADATIONS |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Grad No. | Sieve Size and Percent Passing |  |  |  |  |
|  | 8” | 6” | 4” | 2” | #4 |
| CS 01 | 100 | 97 ± 3 | 90 ± 10 | 45 ± 25 | 20 ± 20 |
| CS 02 |  | 100 | 80 ± 10 | 25 ± 15 |  |

|  | COARSE AGGREGATE SUBGRADE GRADATIONS (Metric) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Grad No. | Sieve Size and Percent Passing |  |  |  |  |
|  | 200 mm | 150 mm | 100 mm | 50 mm | 4.75 mm |
| CS 01 | 100 | 97 ± 3 | 90 ± 10 | 45 ± 25 | 20 ± 20 |
| CS 02 |  | 100 | 80 ± 10 | 25 ± 15 |  |

(2)	The 3 in. (75 mm) capping aggregate shall be gradation CA 6 or CA 10.”

80274