Regional Engineers

Maureen M. Addis

Special Provision for Portland Cement Concrete

August 4, 2017

This special provision was developed by the Central Bureau of Materials to improve uniformity of slump when using a high-range water-reducing admixture.

This special provision should be inserted into all projects involving cast-in-place concrete, precast concrete, and precast prestressed concrete.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the November 17, 2017 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory August 4, 2017.

80389m

# portland cement concrete (bde)

Effective:  November 1, 2017

Revise the Air Content % of Class PP Concrete in Table 1 Classes of Concrete and Mix Design Criteria in Article 1020.04 of the Standard Specifications to read:

| “TABLE 1. CLASSES OF CONCRETE AND MIX DESIGN CRITERIA |  |  |
| --- | --- | --- |
| Class of Conc. | Use | Air Content % |
| PP | Pavement Patching Bridge Deck Patching (10) |  |
|  | PP-1 | 4.0 - 8.0” |
|  | PP-2 |  |
|  | PP-3 |  |
|  | PP-4 |  |
|  | PP-5 |  |

Revise Note (4) at the end of Table 1 Classes of Concrete and Mix Design Criteria in Article 1020.04 of the Standard Specifications to read:

“	(4)	For all classes of concrete, the maximum slump may be increased to 7 in (175 mm) when a high range water-reducing admixture is used.  For Class SC, the maximum slump may be increased to 8 in. (200 mm).  For Class PS, the maximum slump may be increased to 8 1/2 in. (215 mm) if the high range water-reducing admixture is the polycarboxylate type.”

80389