## PORTLAND CEMENT CONCRETE PAVEMENT XX” JOINTED

Revised 2/10/17

The construction of the XX" Portland Cement Concrete Pavement shall be completed as quickly as possible and shall be subject to the (Lane Rental, Intersection Rental, Weekend Closure or other restrictions as appropriate) special provisions.  The mix design shall utilize Class PP concrete criteria and should be based on obtaining a compressive strength of not less than 2000 psi in 24 hours.  Only non-calcium chloride accelerators will be permitted.

The requirements in Article 420.07 paragraph eight regarding use of newly constructed adjacent lanes will be waived, however, the concrete must obtain a strength of not less than 2000 psi before allowing mechanical equipment or traffic on the pavement.  Curing will be maintained until opening strength is attained.  Finishing shall meet the requirements of the Article 420.09; Article 420.09 a(3) and b(3) will be allowed.

DESIGNER NOTES: Use this Spec for new concrete pavement construction at intersections or areas of pavement replacement when the roadway must be reopened to traffic as soon as possible.