G.N.-601

THE HOT-MIX ASPHALT PLUG SHOWN ON HIGHWAY STANDARD 601001 FOR SHOULDER REMOVAL AND REPLACEMENT SHALL BE CONSTRUCTED OF A HOT-MIX ASHPALT MIXTURE OF 75% CA-11 AND 25% CA-16 WITH 2.8 +/- 0.2% OF ASPHALT CEMENT.  THE ASPHALT CEMENT SHALL BE PG-64-22.