G.N.-403

BITUMINOUS SURFACE TREATMENTS: Gradation CA-14 (mid spec.) is assumed for cover coats and gradation CA-16 (mid-spec.) is assumed for seal coats.  The resulting target application rates are as follows:

| TYPE OF CONSTRUCTION | BITUMINOUS MATERIAL | APPLICATION RATE | AGGREGATE | APPLICATION RATE |
| --- | --- | --- | --- | --- |
| Prime Coat (Hard Surface) |  | 0.05 gal/yd2 | FA-1 or FA-2 | 3lb/yd2 |
| Prime Coat (Aggregate Surface) |  | 0.25 gal/yd2* | FA-1 or FA-2 | 4lb/yd2 |
| A-1 |  | 0.35 gal/yd2 | CA-16 | 19lb/yd2 |
| A-2 (Cover Coat) |  | 0.32 gal/yd2 | CA-14 | 25lb/yd2 |
| A-2 (Seal Coat) |  | 0.40 gal/yd2 | CA-16 | 19lb/yd2 |
| A-3 (1st Cover Coat) |  | 0.32 gal/yd2 | CA-14 | 25lb/yd2 |
| A-3 (2nd Cover Coat) |  | 0.45 gal/yd2 | CA-14 | 25lb/yd2 |
| A-3 (Seal Coat) |  | 0.35 gal/yd2 | CA-16 | 19lb/yd2 |

NOTE:  THE ENGINEER RESERVES THE RIGHT TO ADJUST THE TARGET APPLICATION RATES AND THE QUANTITIES.

*Note:  Do not puddle prime.

DESIGN NOTES:  (Design notes shall not appear in the contract.)

- The Bituminous Materials and Application Rates shall be verified with Materials Section in Project Implementation during plan preparation.

- The applicable information on this sheet should be included in the General Notes for the contract.