All District Engineers, Robert Strand, and Thomas R. Walker

William T. Sunley

Special Provision for Grooving Concrete Structures

April 23, 1998

This special provision was developed by the Bureau of Materials and Physical Research based on the latest recommendation of the International Grooving and Grinding Association.  Spacings of 25 mm (1 inch) or greater produce more noise.

The districts should include the BDE Check Sheet with the applicable BDE Special Provisions marked for the July 31, 1998 letting and for subsequent lettings and the Project Development and Implementation Section will include the paper copy in the contract.

This special provision will be transferred through Microsoft Exchange to the district offices on April 23, 1998.

AK:mac\s:\wpdocs\sp\spmemo\21660.doc

Grooving of Concrete Structures (BDE)

Effective:  July 1, 1998

Revise the second sentence of the second paragraph of Article 503.17(c)(4)b to read:

“The Contractor shall have the option of constructing the grooves at either a random spacing of 15 mm (5/8 inch) to 22 mm (7/8 inch) or a uniform spacing of 20 mm (3/4 inch) centers.”

21659