All Regional Engineers

John D. Baranzelli

Special Provision for Bituminous Materials Cost Adjustments

April 19, 2013

This special provision was developed by IDOT and Industry as a result of the volatility in the cost of bituminous materials.  It has been revised to correct an error.

This special provision should be included in projects with at least 1,200 tons (1,100 metric tons) of applicable bituminous work.  The adjustments are applicable to permanent and temporary hot-mix asphalt (HMA) mixtures, bituminous surface treatments (cover and seal coats), and pavement preservation type surface treatments.  The adjustments are not applicable to bituminous prime coats, tack coats, crack filling/sealing, or joint filling/sealing.

This special provision should not be included in alternate pavement bid projects.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the August 2, 2013 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory April 19, 2013.

80173m

# BITUMINOUS MATERIALS COST ADJUSTMENTS (bde) (RETURN FORM WITH BID)

Effective:  November 2, 2006

Revised:  August 1, 2013

Description.  Bituminous material cost adjustments will be made to provide additional compensation to the Contractor, or credit to the Department, for fluctuations in the cost of bituminous materials when optioned by the Contractor.  The adjustments shall apply to permanent and temporary hot-mix asphalt (HMA) mixtures, bituminous surface treatments (cover and seal coats), and preventative maintenance type surface treatments.  The adjustments shall not apply to bituminous prime coats, tack coats, crack filling/sealing, or joint filling/sealing.

The bidder shall indicate on the attached form whether or not this special provision will be part of the contract and submit the completed form with his/her bid.  Failure to submit the form, or failure to fill out the form completely, shall make this contract exempt of bituminous materials cost adjustments.

Method of Adjustment.  Bituminous materials cost adjustments will be computed as follows.

CA = (BPIP - BPIL) x (%ACV  / 100) x Q

Where:	CA	=	Cost Adjustment, $.

BPIP	=	Bituminous Price Index, as published by the Department for the month the work is performed, $/ton ($/metric ton).

BPIL	=	Bituminous Price Index, as published by the Department for the month prior to the letting, $/ton ($/metric ton).

%ACV	=	Percent of virgin Asphalt Cement in the Quantity being adjusted.  For HMA mixtures, the % ACV will be determined from the adjusted job mix formula.  For bituminous materials applied, a performance graded or cutback asphalt will be considered to be 100% ACV and undiluted emulsified asphalt will be considered to be 65% ACV.

Q	=	Authorized construction Quantity, tons (metric tons) (see below).

For HMA mixtures measured in square yards:  Q, tons = A x D x (Gmb x 46.8) / 2000.  For HMA mixtures measured in square meters:  Q, metric tons = A x D x (Gmb x 1) / 1000.  When computing adjustments for full-depth HMA pavement, separate calculations will be made for the binder and surface courses to account for their different Gmb and % ACV.

For bituminous materials measured in gallons:	Q, tons = V x 8.33 lb/gal x SG / 2000

For bituminous materials measured in liters:	Q, metric tons = V x 1.0 kg/L x SG / 1000

Where:	A	=	Area of the HMA mixture, sq yd (sq m).

D	=	Depth of the HMA mixture, in. (mm).

Gmb	=	Average bulk specific gravity of the mixture, from the approved mix design.

V	=	Volume of the bituminous material, gal (L).

SG	=	Specific Gravity of bituminous material as shown on the bill of lading.

Basis of Payment.  Bituminous materials cost adjustments may be positive or negative but will only be made when there is a difference between the BPIL and BPIP in excess of five percent, as calculated by:

Percent Difference = {(BPIL – BPIP) ( BPIL} ( 100

Bituminous materials cost adjustments will be calculated for each calendar month in which applicable bituminous material is placed; and will be paid or deducted when all other contract requirements for the work placed during the month are satisfied.  The adjustments shall not apply during contract time subject to liquidated damages for completion of the entire contract.

Return With Bid

| ILLINOIS DEPARTMENT OF TRANSPORTATION | OPTION FOR BITUMINOUS MATERIALS COST ADJUSTMENTS |
| --- | --- |

The bidder shall submit this completed form with his/her bid.  Failure to submit the form, or failure to fill out the form completely, shall make this contract exempt of bituminous materials cost adjustments.  After award, this form, when submitted, shall become part of the contract.

Contract No.:

Company Name:

Contractor’s Option:

Is your company opting to include this special provision as part of the contract?

Yes			No

Signature:	  Date:

80173