All Regional Engineers

Eric E. Harm

Special Provision for Concrete Gutter, Type A

September 26, 2008

This special provision was developed by the Bureau of Design and Environment to update the design of concrete gutter, Type A to current practice.  It should be inserted into contracts using concrete gutter, Type A.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the January 16, 2009 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory September 26, 2008.

80214m

# CONCRETE GUTTER, TYPE A (BDE)

Effective:  January 1, 2009

Revise the first two paragraphs of Article 606.07 of the Standard Specifications to read:

“	606.07	Concrete Gutter, Curb, and Curb and Gutter.  Joints in concrete gutter, curb, and combination curb and gutter shall be a continuation of the joints in the adjacent portland cement concrete pavement, base course, base course widening, or shoulder.  Expansion joints adjacent to drainage castings may be placed in prolongation with other joint types.

When concrete gutter, curb, and combination curb and gutter are constructed adjacent to flexible pavement or shoulders, joints shall be constructed according to the details shown on the plans.”

Delete the fourth sentence of the fourth paragraph of Article 606.07 of the Standard Specifications.

80214