All Regional Engineers

Scott E. Stitt

Special Provision for Portland Cement Concrete Sidewalk

September 30, 2011

This special provision was developed by the Bureau of Design & Environment to make all expansion joints in sidewalk 1/2 inch and thus comply with ADA requirements.

It should be included in all projects involving the construction of sidewalks or curb ramps.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the January 20, 2012 and subsequent lettings.  The Project Development and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory 
September 30, 2011.

80280m

# PORTLAND CEMENT CONCRETE SIDEWALK (bde)

Effective:  January 1, 2012

Revise Article 424.07 of the Standard Specifications to read:

“	424.07	Expansion Joints.  Expansion joints shall be 1/2 in. (13 mm) thick and consist of preformed joint filler.  The top of the joint filler shall be 1/4 in. (6 mm) below the surface of the sidewalk.

Expansion joints shall be placed in locations as follows.

(a)	Expansion joints shall be placed between the sidewalk and all structures such as light poles, traffic signal poles, traffic poles and subway columns, which extend through the sidewalk.

(b)	Transverse expansion joints shall be placed at maximum intervals of 50 ft (15 m) in the sidewalk.  Where the sidewalk is constructed adjacent to pavement or curb having expansion joints, the expansion joints in the sidewalk shall be placed in line with the adjacent expansion joints as nearly as practicable.

(c)	Expansion joints shall also be placed where the sidewalk abuts existing sidewalks, between driveway pavement and sidewalk, and between sidewalk accessibility ramps and curbs where the ramp abuts a curb.”

80280