# 4X

# DRILL AND GROUT #6 or #8 epoxy coated tie BARS

(Effective April 5, 2024)

Description.  This work consists of furnishing, drilling and grouting #6 or #8 epoxy coated tie bars into existing concrete pavement, concrete shoulders or concrete curb and gutter at the locations shown on plan details.

Materials.

Materials shall be according to the following Articles of Section 1000 - Materials:

Item 									Article/Section

(a) Reinforcement Bars ................................................................................................ 1006.10(2)

(b) Non-Shrink Grout ........................................................................................................ 1024.02

CONSTRUCTION REQUIREMENTS

General.  Bar holes shall be drilled as shown on the plans and parallel to the grade and centerline of the existing PCC pavement/shoulder/curb and gutter with a tolerance of 1/8” in 12”. The drilling operations shall not crack or spall the existing concrete pavement.

- Longitudinal Construction Joint. The #6 epoxy coated tie bars shall be installed using the following method.

- Drilled Holes. Holes shall be drilled into the adjacent PCC pavement, PCC shoulder or PCC curb and gutter with a tolerance of 1/8” in 12” at a spacing of 36”.  The tie bars shall be installed with a nonshrink grout or chemical adhesive providing a minimum pull-out strength as follows.

| Bar Size | Minimum Pull-Out Strength |
| --- | --- |
| #6 | 11,000 lb |

Holes shall be blown clean and dry prior to placing the grout or adhesive. If compressed air is used, the pneumatic tool lubricator shall be bypassed and a filter installed on the discharge valve to keep water and oil out of the lines. The installation shall be with methods and tools conforming to the grout or adhesive manufacturer’s recommendations.

- Transverse Construction Joints.  The #8 epoxy coated tie bars shall be installed using the following method.

- Drilled Holes. Holes shall be drilled into the adjacent PCC pavement with a tolerance of 1/8” in 12” at a spacing of +/- twice the spacing of the existing longitudinal reinforcement.  The tie bars shall be installed with a nonshrink grout or chemical adhesive providing a minimum pull-out strength as follows. The tie bars shall be installed with a nonshrink grout or chemical adhesive providing a minimum pull-out strength as follows.

| Bar Size | Minimum Pull-Out Strength |
| --- | --- |
| #8 | 11,000 lb |

Holes shall be blown clean and dry prior to placing the grout or adhesive. If compressed air is used, the pneumatic tool lubricator shall be bypassed and a filter installed on the discharge valve to keep water and oil out of the lines. The installation shall be with methods and tools conforming to the grout or adhesive manufacturer’s recommendations.

An approved non-shrink grout in accordance with Section 1024 of the Standard Specifications shall be used as the anchoring material for reinforcement bars.

The grout shall be of a consistency such that the bar may be easily inserted into the hole with flow surrounding the bar and without appreciable runout of grout after the bar is fully inserted to the depth as described in plan details.

The grout should be thicker than the consistency recommended by the manufacturer’s directions. The grout shall be injected to the back of the hole to eliminate air pockets prior to inserting the bar. The quantity of material used shall be such that the grout is dispersed along the entire length of the bar and voids are filled. After the material has been positioned at the back of the hole, the bar shall be fully inserted, using a back-and-forth twisting motion, leaving the proper length exposed as shown on the plans.

Method of Measurement.   This work will be measured for payment as follows:

- Contract Quantities.  The requirement for use of contract quantities shall be according to Article 202.07(a) of the Standard Specifications.

- Measured Quantities.  This work shall be measured for payment as each.

Basis of Payment.  This work will be paid for at the contract unit price per each for DRILL AND GROUT #6 TIE BARS or DRILL AND GROUT #8 TIE BARS , which price shall include all labor, materials, and equipment to satisfactorily complete the work.