Regional Engineers

Maureen M. Addis

Special Provision for Temporary Pavement Marking

January 13, 2017

This special provision was developed by the Bureau of Materials and Physical Research and the Bureau of Operations to create a statewide specification for a temporary pavement marking tape with improved retroreflectivity during wet conditions.  This special provision has been revised to pay for the removal of temporary pavement markings separately from permanent pavement markings.

Note:  The title of this special provision has been revised from Pavement Marking Tape Type IV to Temporary Pavement Marking.

This special provision should be inserted into contracts where work zone pavement markings are required.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the April 28, 2017 and subsequent lettings.  The Project Coordination and Implementation Section will include a copy in the contract.

This special provision will be available on the transfer directory 
January 13, 2017

80298m

# temporary pavement marking (bde)

Effective:  April 1, 2012

Revised:  April 1, 2017

Revise Article 703.02 of the Standard Specifications to read:

“	703.02	Materials.  Materials shall be according to the following.

(a)	Pavement Marking Tape, Type I and Type III 	1095.06

(b)	Paint Pavement Markings 	1095.02

(c)	Pavement Marking Tape, Type IV 	1095.11”

Revise the second paragraph of Article 703.05 of the Standard Specifications to read:

“	Type I marking tape or paint shall be used at the option of the Contractor, except paint shall not be applied to the final wearing surface unless authorized by the Engineer for late season applications where tape adhesion would be a problem.  Type III or Type IV marking tape shall be used on the final wearing surface when the temporary pavement marking will conflict with the permanent pavement marking such as on tapers, crossovers and lane shifts.”

Revise Article 703.07 of the Standard Specifications to read:

“	703.07	Basis of Payment.  This work will be paid for as follows.

(a)	Short Term Pavement Marking.  Short term pavement marking will be paid for at the contract unit price per foot (meter) for SHORT TERM PAVEMENT MARKING.  Removal of short term pavement markings will be paid for at the contract unit price per square foot (square meter) for SHORT TERM PAVEMENT MARKING REMOVAL.

(b)	Temporary Pavement Marking.  Where the Contractor has the option of material type, temporary pavement marking will be paid for at the contract unit price per foot (meter) for TEMPORARY PAVEMENT MARKING of the line width specified, and at the contract unit price per square foot (square meter) for TEMPORARY PAVEMENT MARKING LETTERS AND SYMBOLS.

Where the Department specifies the use of pavement marking tape, the Type III or Type IV temporary pavement marking will be paid for at the contract unit price per foot (meter) for PAVEMENT MARKING TAPE, TYPE III or PAVEMENT MARKING TAPE, TYPE IV of the line width specified and at the contract unit price per square feet (square meter) for PAVEMENT MARKING TAPE, TYPE III - LETTERS AND SYMBOLS or PAVEMENT MARKING TAPE, TYPE IV – LETTERS AND SYMBOLS.

Removal of temporary pavement markings will be paid for at the contract unit price per square foot (square meter) for TEMPORARY PAVEMENT MARKING REMOVAL.

When temporary pavement marking is shown on the Standard, the cost of the temporary pavement marking and its removal will be included in the cost of the Standard.”

Add the following to Section 1095 of the Standard Specifications:

“	1095.11	Pavement Marking Tape, Type IV.  The temporary, preformed, patterned markings shall consist of a white or yellow tape with wet retroreflective media incorporated to provide immediate and continuing retroreflection during both wet and dry conditions.  The tape shall be manufactured without the use of heavy metals including lead chromate pigments or other similar, lead-containing chemicals.

The white and yellow Type IV marking tape shall meet the Type III requirements of Article 1095.06 and the following.

(a)	Composition.  The retroreflective pliant polymer pavement markings shall consist of a mixture of high-quality polymeric materials, pigments and glass beads distributed throughout its base cross-sectional area, with a layer of wet retroreflective media bonded to a durable polyurethane topcoat surface.  The patterned surface shall have approximately 40% ± 10% of the surface area raised and presenting a near vertical face to traffic from any direction.  The channels between the raised areas shall be substantially free of exposed beads or particles.

(b)	Retroreflectance.  The white and yellow markings shall meet the following for initial dry and wet retroreflectance.

(1)	Dry Retroreflectance.  Dry retroreflectance shall be measured under dry conditions according to ASTM D 4061 and meet the values described in Article 1095.06 for Type III tape.

(2)	Wet Retroreflectance.  Wet retroreflectance shall be measured under wet conditions according to ASTM E 2177 and meet the values shown in the following table.

Wet Retroreflectance, Initial RL

| Color | RL 1.05/88.76 |
| --- | --- |
| White | 300 |
| Yellow | 200 |

(c)	Color.  The material shall meet the following requirements for daylight reflectance and color, when tested, using a color spectrophotometer with 45 degrees circumferential/zero degree geometry, illuminant D65, and a two degree observer angle.  The color instrument shall measure the visible spectrum from 380 to 720 nm with a wavelength measurement interval and spectral bandpass of 10 nm.

| Color | Daylight Reflectance %Y |
| --- | --- |
| White | 65 minimum |
| *Yellow | 36-59 |

*Shall match Federal 595 Color No. 33538 and the chromaticity limits as follows.

| x | 0.490 | 0.475 | 0.485 | 0.530 |
| --- | --- | --- | --- | --- |
| y | 0.470 | 0.438 | 0.425 | 0.456 |

(d)	Skid Resistance.  The surface of the markings shall provide an average minimum skid resistance of 50 BPN when tested according to ASTM E 303.

(e)	Sampling, Testing, Acceptance, and Certification.  Prior to approval and use of the wet reflective, temporary, removable pavement marking tape, the manufacturer shall submit a notarized certification from an independent laboratory, together with the results of all tests, stating that the material meets the requirements as set forth herein.  The certification test report shall state the lot tested, manufacturer’s name, and date of manufacture.

After approval by the Department, samples and certification by the manufacturer shall be submitted for each batch used.  The manufacturer shall submit a certification stating that the material meets the requirements as set forth herein and is essentially identical to the material sent for qualification.  The certification shall state the lot tested, manufacturer’s name, and date of manufacture.

All costs of testing (other than tests conducted by the Department) shall be borne by the manufacturer.”

80298