# 4Z

# TACK COAT

(Effective December 10, 2025)

Replace the application rate table in Article 406.05 (c)(1) of the Standard Specifications with the following:

| Type of Surface to be Tacked | Residual Asphalt Rate lb/sq ft |
| --- | --- |
| Concrete, Existing HMA, and Milled HMA | .05 |
| New HMA and Brick | .05 |